# FAILURE CRITERIA FOR PREDICTION OF TRANSVERSE MATRIX CRACKING IN COMPOSITES

Pedro P. Camanho

DEMEGI - Faculdade de Engenharia

Universidade do Porto

## Portugal

Carlos G. Dávila

Analytical and Computational Methods Branch

NASA Langley Research Center

Hampton, VA 23681

U.S.A.

## ABSTRACT

## An accurate framework describing the material response caused by the evolving damage state is required for reliable structural integrity analyses of advanced composite structures. The greatest difficulty in the development of an accurate and computationally efficient numerical procedure to predict damage growth has to do with how to analyze the material micro-structural changes and how to relate those changes to the material response.

Several theories have been proposed for predicting failure of composites. While significant progress has been made in this area, there is currently no single theory that accurately predicts failure at all levels of analysis, for all loading conditions, and for all types of fiber reinforced polymer (FRP) laminates. While some failure theories have a physical basis, most theories represent attempts to provide mathematical expressions that give a best fit of the available experimental data in a form that is practical from a designer’s point of view.

To the structural engineer, failure criteria must be applicable at the level of the lamina, the laminate, and the structural component. Failure at these levels is often the consequence of an accumulation of micro-level failure events. Therefore, it is also necessary to have an understanding of micro-level failure mechanisms in order to develop the proper failure theories.

The World Wide Failure Exercise (WWFE) conceived and conducted by Hinton and Soden [1] provides a good picture of the status of currently available theoretical methods for predicting material failure in fiber reinforced polymer composites. The recently published comparison of the predictions by the WWFE participants with experimental results indicates that even when analyzing simple laminates that have been studied extensively over the past 40 years, the predictions of most theories differ significantly from the experimental observations.

The uncertainty in the prediction of initiation and progression of damage in composites has led to the undertaking of an effort to revisit existing failure theories and to develop new ones where necessary. The well-established failure criteria were revisited and their prediction capabilities were compared and their qualities were examined.

This paper describes part of a newly developed set of non-empirical criteria for predicting the different failure modes of unidirectional FRP laminates (LaRC03 Failure Criteria). All the calculations are at the lamina level with plane stress assumptions.

The proposed failure criterion for matrix failure under in-plane shear and transverse tension is based on Fracture Mechanics analyses of cracked plies. The proposed criterion can predict the increased strength of a ply when it is embedded in a laminate, and when its thickness decreases (in-situ effect).

Figure 1 shows the comparison between the predicted results and published experimental results for AS4-55A carbon fiber reinforced composites. Other examples of failure envelopes for different materials under several load conditions will be presented.

Figure 1- Comparison between LaRC03 failure criterion and published experimental data.

REFERENCES

[1]	Soden, P.D., Hinton, M.J., Kaddour, A.S., "A Comparison of the Predictive Capabilities of Current Failure Theories for Composite Laminates", Composites Science and Technology, Vol. 58, No. 7, pp. 1225-1254, 1998.

# Text boxes

Experimental data